###### UNIVERSAL LEATHER OIL

Universal leather oil is for use in perchloroethylene and hydrocarbon. It can be used in the machine and for over-spraying already dry-cleaned garments. Buying Universal Leather Oil means you need only keep one oil in stock.

Instructions

For a two bath process, clean with Sultrasoft HC ( around 2-3mls per litre of solvent) for around 5 minutes. Follow this with a distilled rinse.

Following this  we recommend that a 2 to 4 % solution is made up of Universal Leather oil, ( 20 to 40ml per litre of solvent)  this rate depends on the degreasing effect that has taken place. This should be for around 7 minutes for light colours down to 4-5 mins for dark colours.

Use as small a dip of solvent as possible for reasons of economy.  Rinse

For application by spraying we recommend that Universal Leather Oil be mixed with about seven parts of water prior to being sprayed on to garments.

Correctly used Universal Leather Oil will enrich the skin and deepen the colour. After spraying will also subdue minor patchyness caused in the cleaning process.

# Text boxes

# PRODUCT

INFORMATION